|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| **3D-printed samples** | ***C. albicans*** (CFU/sample) | | | |
| **1.run** | **2. run** | **3. run** | **Mean** |
| Control | 266 | 465 | 172 | 301 |
| Experimental | 882 | 1817 | 1907 | 1535 |

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| **Heat-cured samples** | ***C. albicans*** (CFU/sample) | | | |
| **1.run** | **2. run** | **3. run** | **Mean** |
| Control | 0 | 0 | 0 | 0 |
| Experimental | 302 | 324 | 315 | 314 |